## Slide 1: Technology development for OPCPA multi-PW laser system
Marco Galimberti
Central Laser Facility
Science and Technology Facilities Council
Rutherford Appleton Laboratory

## Slide 2: Summary
Vulcan 10PW (now 20PW) Project
Technology Development Plan
Conclusion

## Slide 3: Vulcan 10PW Project
600 J
Additional Vulcan
2 x 1.2 kJ 3 ns
208 beam lines
1x 30J small beamline
SHG
527 nm
527 nm
SHG
KD*P
KD*P
KD*P
kJ OPCPA amplification stages
SHG
527 nm 12J
600 J
Compressor
300 J , 30 fs
>500 J
Beam propagation to HIA
High Intensity Area
HIA
10 PW + KJ long pulse
Target area Petawatt
TAP 10
1 PW + 10 PW
Beam propagation to TAP 10
Existing Vulcan beam lines
I. N. Ross et al., Opt. Commun. 144, 125 (1997)
A. Dubietis et al., Opt. Commun. 88, 437 (1992)
Based on a combination of LBO and KD*P using OPCPA
Crystal- KD*P, Largest available
Meets aperture requirement BW >150 nm
Implies 910 nm operation
OPCPA Pump laser
10 PW Front End
1J, 910nm, 150nm BW 3ns
Seed generation
Stretch
OPCPAs (LBO) 1J amplification

## Slide 4: K*DP - Small Signal Gain
10PW
Non-colinear
colinear
20PW

## Slide 5: DKDP 80%
Shortest pulse achievable:
FWHM = 11.4 fs
Three stages simulations

## Slide 6: 20PW Specifications
Partially Deuterated KDP (80%)
Central wavelength: 957nm
Bandwidth: 220nm
Final Energy: 400J
Pulse Length: 20fs

## Slide 7: Technology Development Plan
Component Test Lab
High deuterated DKDP Crystals
Coherent Beam Recombination
Coatings
High Repetition Rate Disk Amplifier
Gratings

## Slide 8: Component Test Lab
Broad band Seed pulse ~1 J λ=910nm
Existing 10 PW Front End
OPCPA stages based on LBO
New Amplification stage based on DKDP
Output: ~6J
S=910nm
 ~150nm
Pump: 15J
P=527nm
∆T=3 ns
Frequency Doubling and OPCPA
Layout Scalable to Large Aperture

## Slide 9: SHG Conversion Efficiency
Referred to Green Energy on the OPCPA Crystal

## Slide 10: Small DKDP Crystal Tests
80% deuteration DKDP Crystal spec | 
Deuteration level | 80(+/- 1)%
Transmitted measured wavefront | <Lambda/10
TWF Gradients | <Lambda/4/cm
Dimensions | 50x50x64 mm
Will test three crystals
80% deuteration - Slow grow method
87% deuteration
100% deuteration

## Slide 11: Phase Matching K*DP 80%
Used cylindrical lens on both the signal and pump beams to find the phase matching angle.
Position of stripe moves with crystal angle, phase matching achieved when stripe is in centre of near field.
Signal Near Fields

## Slide 12: Amplification
With 40mJ incident have achieved 0.9J with 16J in the green.
Green trace amplified
Red trace seed
Near-field image of signal.
Double image due to coatings.
Can see some damage to mirrors at top
Wavelength [nm]
Intensity [A.U.]

## Slide 13: Coherent beam recombination

## Slide 14: Gemini laser facility
Two synchronised CPA beams, independently configurable
    Energy on Target 15 J
    Pulse Duration on Target 30 fs
    Focal Spot Size 2 mm
    On Target intensity 1021 W/cm2
    Shot Repetition Rate 20 seconds
    Pulse contrast (ASE) 1010

## Slide 15: Gemini Experiment
OAP 1
OAP 2
Beam 1
Beam 2
Serrated D-Shaped apertures installed before VSF to compressors
Diagnostics
150mm

## Slide 16: Results
Beams 1 and 2 pointing stability
Problem identified on the experimental campaign:
Beam pointing stability need to be improved;
Relative phase between the two beam need to be stabilized actively;
Alternative relative phase measurement should be investigated.
In Phase
π Phase

## Slide 17: Current development
Loop Off
2s
Loop On
2s
A new laboratory has been setup.
The layout is more similar to the Gemini experiment.
Develop fast beam pointing stabilisation using relatively large (50mm) piezo driven mirror
Develop relative phase measurement and stabilization loop between the beams

## Slide 18: Conclusion
With the work done so far we are confident to be able to achieve 20PW
Currently under testing different partial deuterated crystals
We are working on the technology for the 100PW class lasers